## Slide 1: Week 2, Lattice Vibration, Phonons
Quantum harmonic oscillator, vibration of molecules, normal modes, lattice phonon waves, second quantization, lattice dynamics, phonon dispersion from DFT first principles

## Slide 2: Harmonic oscillator
x
x
E
Notes: Review the quantum-mechanics books, such as J. J. Sakurai.

## Slide 3: Annihilation and creation operators
Energy E
E
Notes: Note, we follow the usual convention of Dirac <f | g> = (g, f), i.e., linear in g, antilinear in f, and adjunct (Hermitian) is defined by ( a g, f) = (g, a^+ f).

## Slide 4: Molecular vibration, normal mode
Notes: Q_n(t) = Q_n exp(-I w_n t) is called the normal mode coordinate for the mode n.

## Slide 5: Water molecule
O
H
H
Notes: From page 10 in https://www.princeton.edu/~fhs/fhspapers/fhspaper79.pdf

## Slide 6: Molecular vibration, group theory, H2O
C2v |  | E | C2 | v | ’v
z | A1 | 1 | 1 | 1 | 1
Rz | A2 | 1 | 1 | -1 | -1
x, Ry | B1 | 1 | -1 | 1 | -1
y, Rx | B2 | 1 | -1 | -1 | 1
 | a.s | 3 | 1 | 3 | 1
A1 A1
B1
x
z
Notes: See chap 8 of Dresselhaus et al, “Group theory, application to physics of condensed matter” sigma_v, in the plane of molecule, sigma_v’ is perpendicular to the plane of molecule. C2 (z axis) passes through O, in the plane of molecule, in the direction of two Hs.

## Slide 7: Direct product representation
Notes: N here is the order of the group.

## Slide 8: Lattice vibration, 1D chain
a: lattice constant
x0
xl-1 xl xl+1
k k
xN-1 xN =x0
0
2/a
q


## Slide 9: Normal mode coordinates, second quantization of 1D chain
Notes: Lattice vibration differs from small molecules in that here we deal with travelling wave instead of standing wave.

## Slide 10: 1D chain with two kinds of atoms
k k k
M1 M2
a
q
/a

l-1 l l+1
LA
LO
Notes: (u1,u2) is (e1, e2) except e is normalized to 1, i.e., e^+ e = 1.

## Slide 11: General lattice, forces, eqn
a1
a2
Rl
rj
xlj
Notes: For general discussion of phonon physics, see e.g., J Callaway, “Quantum theory of solid state”.

## Slide 12: Dynamic matrix
Notes: See M Born and K. Huang, “Dynamical Theory of Crystal Lattices”, Clarendon (1954), pages 67-69, 173-175.

## Slide 13: Diamond lattice, structure
Space group Fdm (No. 227) (nonsymmorphic)
Point group Oh (m3m)
Two fcc displaced along (1,1,1) by 1/4 lattice constant
Notes: This page at the bottom give a table of all the 192 space group symmetry operations.
http://lampx.tugraz.at/~hadley/ss1/crystalstructure/structures/diamond/diamond.php
Figure from https://www.researchgate.net/figure/Conventional-cubic-cell-of-the-diamond-lattice-Element-Lattice-Constant-a-A_fig2_285014517

## Slide 14: Character  table for Oh
 | E | 8C3 | 6C2 | 6C4 | 3C2 =(C4)2 | i | 6S4 | 8S6 | 3σh | 6σd | linear, rotations | quadratic
A1g (1) | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 |  | x2+y2+z2
A2g (2) | 1 | 1 | -1 | -1 | 1 | 1 | -1 | 1 | 1 | -1 |  | 
Eg (12) | 2 | -1 | 0 | 0 | 2 | 2 | 0 | -1 | 2 | 0 |  | (2z2-x2-y2, x2-y2)
T1g (15) | 3 | 0 | -1 | 1 | -1 | 3 | 1 | 0 | -1 | -1 | (Rx, Ry, Rz) | 
T2g (25) | 3 | 0 | 1 | -1 | -1 | 3 | -1 | 0 | -1 | 1 |  | (xz, yz, xy)
A1u (1) | 1 | 1 | 1 | 1 | 1 | -1 | -1 | -1 | -1 | -1 |  | 
A2u (2) | 1 | 1 | -1 | -1 | 1 | -1 | 1 | -1 | -1 | 1 |  | 
Eu (12) | 2 | -1 | 0 | 0 | 2 | -2 | 0 | 1 | -2 | 0 |  | 
T1u (15) | 3 | 0 | -1 | 1 | -1 | -3 | -1 | 0 | 1 | 1 | (x, y, z) | 
T2u (25) | 3 | 0 | 1 | -1 | -1 | -3 | 1 | 0 | 1 | -1 |  | 
Notes: See this page for the point group O_h:
http://gernot-katzers-spice-pages.com/character_tables/Oh.html
See also the Wikipedia page for a complete list: https://en.wikipedia.org/wiki/List_of_character_tables_for_chemically_important_3D_point_groups

## Slide 15: Run QE at HPC (e.g., atlas9.nus.edu.sg)
Setup the proper running environment for QE by issuing two linux commands:
source /etc/profile.d/rec_modules.sh
module load espresso6.5-Centos6_Intel
The QE binary is then available as pw.x (for DFT plane wave self consistency) and ph.x (DFT perturbative phonon calculation)
Notes: See HPC site at https://nusit.nus.edu.sg/services/getting-started/introductory-guide-for-new-hpc-users/
Software in general https://nusit.nus.edu.sg/services/hpc/application-software/
and Quantum Espresso in particular https://nusit.nus.edu.sg/services/hpc/application-software/quantum-espresso/

## Slide 16: Quantum Espresso (QE) for phonon mode at  point
Step 1: run pw.x at the equilibrium structure
mpirun –np 8 pw.x –in scf.in > out
Step 2: run ph.x to obtain frequencies and eigenmodes.
mpirun –np 8 ph.x –in ph.in > phout
See also https://www.quantum-espresso.org/resources/tutorials/shanghai-2013/hands-on-phonons/phonons_tutorial_shanghai1.pdf
Notes: See also:
https://www.quantum-espresso.org/resources/tutorials/shanghai-2013/hands-on-phonons/phonons_tutorial_shanghai1.pdf

## Slide 17: Input file scf.in for pw.x
&control
prefix = 'diamond'
calculation = 'vc-relax'
restart_mode = 'from_scratch'
pseudo_dir = './'
/
&system
ibrav = 0
celldm(1)=6.75870348
nat = 2
ntyp = 1
ecutwfc = 60.0
/
&electrons
conv_thr = 1.0d-10
/
&IONS
ion_dynamics = 'bfgs'
/
&CELL
cell_dynamics = 'bfgs'
cell_dofree = 'ibrav'
/
CELL_PARAMETERS alat
0.0000000 0.5000000 0.5000000
0.5000000 0.0000000 0.5000000
0.5000000 0.5000000 0.0000000
ATOMIC_SPECIES
C 12.011 C.UPF
ATOMIC_POSITIONS alat
C 0.0000000 0.0000000 0.000000
C 0.250000 0.25000000 0.250000
K_POINTS automatic
10 10 10 0 0 0

## Slide 18: Input file ph.in for ph.x
phonons at Gamma point
&INPUTPH
prefix = 'diamond'
epsil = .true.
fildyn = 'dyn.G'
tr2_ph = 1.0d-14
/
0.0 0.0 0.0
The normal mode displacements are reported in the dyn.G file.

## Slide 19: Phonon dispersion for diamond
Three units in common use for frequency
1 THz (/(2)) = 33.356 cm-1 (/(2c)) = 4.14 meV (
Notes: Figure from http://exciting-code.org/lithium-phonon-and-thermal-properties-diamond
https://www.researchgate.net/figure/The-Brillouin-zone-of-a-FCC-lattice-Fig-13-The-truncated-octahedron-is-formed-buy_fig3_264872465