## Slide 1: Enhancing thermoelectric efficiency for nanostructures and quantum dots
Jian-Sheng Wang
Department of Physics, National University of Singapore

## Slide 2: Outline
Seebeck effect & thermoelectric efficiency
Disordered graphene/graphane
Quantum master equation: electron-phonon interaction to thermoelectric efficiency in quantum dots
Enhancing thermoelectric efficiency by time-dependent driven
Conclusion
1st Conference on condensed matter physics, 15-17 July 2015

## Slide 3: Seebeck effect
Seebeck coefficient: how much voltage difference can one generate per temperature difference? S =  dV/dT
How efficient is it comparing to Carnot engine, W/Q = 1 – Tc/Th?
Ans: Determined by a material parameter called
ZT = S2T/
 : electric conductivity,  : thermal conductivity, T: absolute temperature
From “Physics Today,” June 2014, p.14

## Slide 4: Enhancing ZT by disordering
Ni, Liang, Wang & Li, Appl. Phys. Lett. 95, 192114 (2009).
ZT at 300K for graphene/graphane calculated using ballistic NEGF formulation for the armchair ribbons with fraction of H-bond disorder, with DFT structure determination.
graphane
graphene
Notes: Different samples for lengths, circle : 3 rings, triangle 5 rings, square 10 hexagonal rings.

## Slide 5: Quantum dot electron-phonon interaction
Model:
Notes: NR: nano-mechanical resonator, SET: single electron transistor.

## Slide 6: Quantum Master equation approach
Advantage of NEGF: any strength of system-bath coupling V; disadvantage: difficult to deal with nonlinear systems.
QME: advantage - center can be any form of Hamiltonian, in particular, nonlinear systems; disadvantage: weak system-bath coupling, small system.
Can we improve?
Wang, et al, Front. Phys. 9, 673 (2014); Thingna, et al, J. Chem. Phys. (2014)

## Slide 7: Dyson Expansions
Notes: Some detail is in the last section of J.-S. Wang, B. K. Agarwalla, H. Li, and J. Thingna, “Nonequilibrium Green's function method for quantum thermal transport,” Front. Phys. (2013). rho_0 is in fact rho_0^I, i.e., interaction picture one.

## Slide 8: Divergence

## Slide 9: Unique one-to-one map, 0↔; ordered cumulants

## Slide 10: Order-by-Order Solution

## Slide 11: Time-dependent driven
Nonequilibrium Green’s function (NEGF), we use Jauho, Wingreen, Meir (PRB 1994) theory
Master equation case - drive change the eigenvalues but not eigenvectors, easily generalize

## Slide 12: Electron current
Zhou, et al, Phys Rev B 90, 045410 (2015).
Electron current in units of . Background temperature , lead temperature , , . . Chemical potentials set to 0 for all leads.
Notice the current changes direction with gate voltage.

## Slide 13: Reduction of ZT under electron-phonon interaction
ZT vs ep interaction strength , for different gate voltage .
back-action (deviation from equilibrium).

## Slide 14: Why drive the system? can have higher efficiency
Far from thermal equilibrium
Break down of Onsager relation (due to break down of time translational invariance)

## Slide 15: How to quantify efficiency in time-dependent situation?
T or 
Current I
Do this analysis for each fixed t.

## Slide 16: Measuring efficiency
See, eg., H J Goldsmid, “Intro to thermoelectricity.”
Optimal efficiency in steady state by maximizing , one obtain
Work done to load
Entropy flow
Peltier heat
Joule heat flow back

## Slide 17: Efficiency enhancement by driven
Zhou, et al, arXiv:1505.06132
Ballistic quantum dot:
Under step control of the drive . (a) efficiency,
(b) Onsager relation broken-down,
(c) entropy flow.

## Slide 18
With ep interaction, arXiv:1505.06132
Wave form of drive.
Entropy transport
Breakdown of Onsager relation
Displacement current
Normalized efficiency

## Slide 19: Summary
Structure change does bring in higher ZT, e.g., disorder, or go down to 0-dimension (quantum dot)
Electron-phonon interaction reduces ZT
Dynamic drive (forcing) improves ZT, up to a factor of 4

## Slide 20: acknowledgements
Students: Hangbo Zhou, Juzar Thingna, Xiaoxi Ni
Collaborators: Peter Hänggi, Baowen Li, Albert Liang GC

## Slide 21: Thank you